## Slide 1: Open Questions in Organometal Halide Perovskites: Ferroelectricity, Ion migration, and Long carrier lifetime
Andrew M. Rappe The Makineni Theoretical Laboratories Department of Chemistry University of Pennsylvania

## Slide 2
High power conversion efficiency (PCE) reached 20% in 2015! (Best silicon solar cell has PCE around 26%)
Fast improvement PCE increased from 9% to 20% within two years
Cheap to make abundant elements  Pb, I, C, N, H easy to make <$1/m2 (Silicon > $10/m2)
Sci. Rep. 2, 591 (2012), Science 345, 542 (2014), Nature 501, 395 (2013)
Device
OMHPs as High Efficiency Solar Cell
C
I
N
Pb
~6.3Å
Unit cell of CH3NH3PbI3 (MAPbI3)
OMHP: Organometal Halide Perovskite
e-
h+
MAPbI3

## Slide 3
Polar order The A-site organic molecule has permanent dipole moment. Is MAPbI3 ferroelectric?
Current-Voltage (J-V) hysteresis The origin is not fully clear.
Ferroelectricity? Trap states at interface/surface? Ion migration?
Carrier lifetime MAPbI3 has exceptionally long carrier life time.
The intrinsic origin remains elusive.
Many Things are Unknown …
Understanding these properties is essential to further optimize OMHP-based solar cells

## Slide 4
Polar order: Ferroelectricity?
XRD and Raman spectra demonstrate no inversion symmetry J. Phys. Chem. Lett. 5, 3937 (2014), Inorg. Chem. 52, 9019 (2013)
Polarization–Electric field (P-E) loop measurement J. Phys. Chem. Lett. 5, 3937 (2014)
Piezoelectric Force Microscopy (PFM) observed switchable ferroelectric domains J. Phys. Chem. Lett. 5, 3335 (2014), J. Mater. Chem. A 3, 7699 (2015), J. Phys. Chem. Lett. 6, 1729 (2015)
J. Phys. Chem. Lett. 5, 3335 (2014)
J. Mater. Chem. A 3, 7699 (2015)
Yes, MAPbI3 may be ferroelectric
Piezoresponse Hysteresis
Ferroelectric domains

## Slide 5
PFM and P-E hysteresis do not support ferroelectric polarization directly Nat. Mater. 14, 193 (2015)
P-E and I-E hysteresis do not show ferroelectricity (large leakage current) J. Phys. Chem. Lett. 6, 1155 (2015)
P-E hysteresis observe huge polarization (>1000µC/cm2) Non-ferroelectric process (e.g., ion migration). is dominant. Appl. Phys. Lett. 106, 173502 (2015)
Au/BiFeO3(260 nm thick)/SrRuO3
Au/MAPbI3/PEDOT:PSS/ITO
No, MAPbI3 may not be ferroelectric
I/E and P/E hysteresis measurements
Polar order: Ferroelectricity?
MAPbI3
BiFeO3
Conflicting experimental observations:
Notes: Nat. Mater. 14, 193 (2015) is from Prof. Jingsong Huang
The graph shows the comparison between MAPbI3 and a typical ferroelectrics BFO. By showing I/E and P/E hysteresis, MAPbI3 shows very different features compared to BFO, indicating that MAPbI3 is not ferroelectric.

## Slide 6
Different scan rates give different results (using PFM) Low scan rate: “No ferroelectricity” Fast scan rate: “Yes ferroelectricity”  poor polarization retention/coercivity. On the time scale around 1 s. J. Phys. Chem. Lett. 6, 1408 (2015)
Crystal size affects polarization retention. Large crystal shows longer retention J. Phys. Chem. Lett. 6, 1729 (2015)
Piezo-phase hysteresis performed at different acquisition times
Ferroelectricity in MAPbI3 depends on experimental setup not robust ferroelectricity, may exhibit voltage-induced local polarization
Polar order: Ferroelectricity?
More conflicting experimental observations:

## Slide 7
A Site Molecule and Ferroelectricity
A site MA+ has permanent dipole moment, which may induce different polar order - Randomly oriented  Paraelecric - Aligned  Ferroelectric - Anti-aligned  Anti-ferroelectric
A site molecules may form specific spatial distribution - Locally ordered nano-domains - Ferroelectric domains and domain walls
A lot of effort devoted to understanding molecular behaviors - Time-dependent permittivity measurement J. Appl. Phys. 87, 6373 (1987) - Neutron powder diffraction Chem. Commun. 51, 4180 (2015) - Quasielastic neutron scattering Nat. Comm. 6, 7124 (2015) - ab initio molecular dynamics Phys. Chem. Chem. Phys. 16, 16137 (2014) - Monte-Carlo simulation APL Mat. 2, 081506 (2014) - …
P
-
+
2.2D
Study molecular behaviors is important for understanding Ferroelectricity
C
N

## Slide 8
Behavior of A Site Molecule
Quasielastic Neutron Scattering + Monte Carlo
Residence time for MA+ orientation is around 14±3 ps. (consistent with previous ab initio MD)
Rotation barrier is on the level of 10 meV. (estimated from Arrhenius activity energy)
Suspect that MA+ in ferroelectric domain may have larger rotation barrier (longer residence time)
Nat. Comm. 6, 7124 (2015)
180˚ rotation
(i) and (ii) are unlike to occur in the time scale 1.2~53 ps
Other rotation patterns are possible
Complete random

## Slide 9
Monte-Carlo Simulation
K = 25 meV
28 nm×28nm×7.5 nm
K = 100 meV
Ferroelectric domains can form @ RT
Dipole-dipole interaction
Value of K estimated from
DFT, favors aligned dipoles
Antiferroelectric domains
Ferroelectric domains
Notes: The plotted 3D domain graph here is the simulation cooling to 50K. But ferroelectric domain can exist even >350 K from the simulation.

## Slide 10
Bulk photovoltaic effect (BPVE)
Intrinsically generated photocurrents and photovoltages from single phase bulk material
Observed in experiments:
  Inversion symmetry breaking
  Maybe parallel, antiparallel,
  or even perpendicular
  to material polarization
  Strong frequency dependence
  Shift current is the main mechanism for BPVE
BaTiO3
S. M. Young and A.M. Rappe, Phys. Rev. Lett., 109, 116101 (2013)
S. M. Young, F. Zheng, and A. M. Rappe, Phys. Rev. Lett., 109, 236601 (2013)
V. I. Belinicher and B. I. Sturman, Sov. Phys. Usp. 23(3), 199 (1980)

## Slide 11
Shift Current
Transition intensity
Shift vector
Phys. Rev. B. 23, 5590 (1981), Phys. Rev. B. 61, 5337 (2000)
Quadratic in E field, linear in light intensity!
Need to break inversion symmetry
Rank 3 tensor

## Slide 12
Shift Current in MAPbI3
5 μC/cm2 Polarization Along c
Large Pb-I3 displacement Polar
Near Net Zero Polarization Small Pb-I3 displacement Non-polar
Bulk photovoltaic effect emerges when system loses inversion symmetry Shift current effect on two cases: Polar & Non-polar

## Slide 13
Higher response than BiFeO3 (BFO)
BFO
BFO Eg=2.74 eV
zzZ
BFO
zzZ
Shift Current in MAPbI3
Higher response than BFO may explain large Voc
Polar (M1) gives larger response than Non-polar (M2)
J. Phys. Chem. Lett. 6, 31 (2015)
Shift current (thin limit)
Glass coefficient (thick limit)
Notes: By saying that shift current may also explain the I/V hysteresis, the next section about hysteresis can start more naturally.

## Slide 14
Current-Voltage Hysteresis
J-V curve
Anomalous hysteresis in MAPbIxCl1-x
Power conversion efficiency:
The rise time to reach stabilized power output is slow
Determination of PEC is ambiguous
J-V curve is sensitive to experimental conditions
FB: Forward Bias; SC: Short Circuit
J. Phys. Chem. Lett 5, 1511 (2014)

## Slide 15
Parameters affecting J-V Hysteresis
Scanning rate
Interface
Crystal size
Aging
Solar cell architecture
Mesoporous TiO2
Mesoporous Al2O3
J. Phys. Chem. Lett 5, 1511 (2014)
J. Phys. Chem. Lett 5, 2927 (2014)
Energy Environ. Sci., 8, 995 (2015)

## Slide 16
Possible Origins of J-V Hysteresis
Trap states at interface/surface
Ferroelectricity: remnant polarization
Bulk photovoltaic: large Voc
Ion migration
Light-induced structural transformation
Ultraviolet photoemission spectra for CH3NH3PbI3 thin films vapor deposited on native oxide terminated silicon from PbI2 (blue) and PbCl2 (red) precursors.
Trap states at surface
Ferroelectric domains
Light-enhanced piezoelectricity
J. Phys. Chem. Lett 6, 1408 (2015)
J. Phys. Chem. Lett 5, 3335 (2014)
J. Am. Chem. Soc. 137, 2089 (2015)

## Slide 17
Ion Migration in OMHP
Giant switchable photovoltaic effect
Photoinduced giant dielectric constant
J. Phys. Chem. Lett 5, 2390 (2014)
Low frequency
Angew. Chem. Int. Ed. 54, 1 (2015)
Low frequency
The ionic diffusion is highly relevant for J-V hysteresis, ionic conductivity, low-frequency dielectric response, and material stability.
σ: conductivity; ε: dielectric constant
Nature Mater. 14, 193 (2015)
Significant ionic conductivity
σion > σele
σ
εr,∞

## Slide 18
  2×2×1 super-cell of MAPbI3, 16 formula units
  PBE-DFT + dispersive corrections in VASP
  nudged elastic band (NEB) using VTST
  different charge states of hydrogen:
  H+, H0, H-
  modeled by fixing the number of electrons per cell
  sample a slice of lateral adiabatic potential energy surface
Hydrogen in MAPbI3: Structural Model
D. A. Egger, L. Kronik, A. M. Rappe, Angew. Chem. Int. Ed. 2015, online

## Slide 19
All three hydrogenic defects are found to be repelled from the A site
H+ is stable in the vicinity of I
H0 is in an interstitial Pb-I site
H- is closer to the Pb site
Ionic character MAPbI3
Adiabatic PES of Hydrogen in MAPbI3

## Slide 20
energy
I Pb I
H+
H-
H-
Bourgoin-Corbett mechanism:1 interstitial migrates via successive changes of its charge state
Similar mechanism relevant for Si-interstitials in Si2,3  might be relevant for other defect types too
1 Bourgoin & Corbett, Phys. Lett. 38A, 2 (1971)
2 Bar-Yam and Joannopoulos, Phys. Rev. Lett. 52, 1129 (1984);
3 Car et al., Phys. Rev. Lett. 52, 1814 (1984)
Ionization enhanced hydrogen migration
Trap states at surface

## Slide 21
0.29 eV
Overall proton migration is enhanced by successive displacements of iodide atoms.
The energy barriers for iodide-iodide H+ transfer can even be as low as 0.17 eV if proton migration between different I sites is considered
Minimum energy path for H+ in MAPbI3
Proton migration between equatorial iodines in MAPbI3

## Slide 22
Science 342, 341 (2013)
Science 342, 344 (2013)
Observation of Long Carrier Lifetimes
LD =1069 nm
τ = 273 ns
LD =129 nm
τ = 9.6 ns
Legend: 1ps 100 ps 500 ps 1 ns
Photoluminescence
Transient Absorption

## Slide 23
Explanation of Long Carrier Lifetimes (1)
Defects with favorable formation energies have shallow levels  Electronically benign
Adv. Mater. 26, 4653 (2014)
J. Phys. Chem. C, 119 , 5253 (2015)
Angew. Chem. 54, 1791 (2015)

## Slide 24
Explanation of Long Carrier Lifetimes (2)
Charge separation induced by long range potential fluctuations associated with molecular orientational disorder.
Large scale DFT calculations suggest that the localization length is 40 – 60 nm.
Nano Lett. 15, 248 (2015)

## Slide 25
Explanation of Long Carrier Lifetimes (3)
111 molecular orientation
011 molecular orientation
Dynamical band gap: CBM position fluctuates at room temperature
Nat. Comm. 6, 7026 (2015)

## Slide 26
Domain Walls and Carrier Lifetimes
Potential steps from domain walls aid carrier separation
Carriers move along potential maxima in multi-domain samples
J. Phys. Chem. Lett., 6, 693 (2015)
Nano Lett. 14, 2584 (2014)
Domain wall  Polarization gradient  Built-in electric field

## Slide 27
CBM is located at domain wall A: Pz components meeting with a head-to-head configuration
VBM is located at domain wall B: Pz components meeting with a tail-to-tail configuration
Domain Walls and Carrier Lifetimes
S. Liu et al., J. Phys. Chem. Lett., 6, 693 (2015)
Layer-resolved local density of states
Electronic electrostatic potential

## Slide 28
Spin Effects on Carrier Lifetimes
Favorable spin helicity
Unfavorable spin helicity
S=-1
s=+1
Spin-forbidden transition
Spin-allowed transition
CS= +1
VS= -1
CS= +1
VS= +1
Favorable and unfavorable spin helicities
Spin helicity can be controlled by structural distortions

## Slide 29
Space group: I4cm, Room temperature
Spin Effects on Carrier Lifetimes
Pb displacements give rise to favorable spin helicity
F. Zheng et al, submitted (2015)

## Slide 30
Materials design: Halide Substitution
Chung et al., Nature 485,486 (2012)
Stranks et al., Science 342, 341 (2013)
Halide substitution has significant impact on efficiencies
What are the materials design principles?
  Theoretical guidance is needed.

## Slide 31
Equatorial Substitution
Apical
Substitution
Structure | ¦Pz¦ (μC/cm2) | Band Gap, SOC (eV)
CH3NH3PbI3 | 5.0 | 0.69
CH3NH3PbI3-xClx , equatorial | 6.2 | 0.83
CH3NH3PbI3-xClx , apical | 4.4 | 0.84
Materials design: Halide Substitution
Atomic structure of CH3NH3PbI3-xClx
J. Phys. Chem. Lett. 6, 31 (2015)

## Slide 32: Glass coefficient response of MAPbI3-xClx M1 Structures (polar)
Cl substitution increases response in some cases
Equatorial site substitution gives larger response
Indicate maximum CH3NH3PbI3 M1 response
zzZ
M1: net dipole along z
Enhancement due to Cl doping

## Slide 33
Summary
Ferroelectricity in OMHPs is in debate: - Experimental setup may strongly affect the ferroelectricity - A site molecular dynamics is important for understanding the ferroelectricity - Bulk photovoltaic effect in polar order has higher magnitude than BiFeO3, which may explain the large Voc.
Origin of J/V hysteresis is still unknown: - Ion migration may play an important role in J/V hysteresis - Hydrogen migration in MAPbI3 is studied systematically
Intrinsic reason of long carrier lifetime: - Low defect density; disordered dynamics of molecules; … - Domain and domain wall can help separate carriers - Rashba spin helicity plays a significant role in explaining long carrier lifetime

## Slide 34
Acknowledgments
Funding agencies:
DOE
ONR
NSF
Computational resources:
DOE/NERSC
DOD/HPCMP
Collaborators:
Shift Current: F.Zheng, H.Takenaka, F.Wang, N.Z.Koocher
Domain walls: S.Liu, F.Zheng, N.Z.Koocher, H.Takenaka, F.Wang
H Diffusion: D. Egger, L. Kronik
Rashba/lifetime: F.Zheng, L.Z.Tan, S. Liu