## Slide 1: Metamaterials-Inspired Electromagnetics and Photonics
Gennady Shvets, The University of Texas at Austin
Condensed Matter and Materials Research Committee Spring Meeting, National Academies’ Keck Center, Washington, DC, May 1, 2014

## Slide 2: Meta-Materials: Mesoscopic EM Materials
Unit cell is small enough effective medium description (homogenization, constitutive parameters e, m)
Carefully designed resonant unit cells (e.g. split rings etc.)
Remarkable optical/EM properties enabled by finite cell size  spatial dispersion, optical magnetism, bi-anisotropy
Natural materials: unit cell is an atom << radiation wavelength
Photonic crystals: unit cell is sized to ½ of the radiation wavelength
MetaMaterials: atom << unit cell < l

## Slide 3: Evolution of Metamaterials Research
Early days: focus on exotic bulk properties  negative refractive index, super-lensing, “cloaking”
Understanding of the EM properties of MMs and their building blocks: high-frequency magnetism, bi-anisotropy, homogenization
Modern Era: Metamaterials-inspired Electromagnetics in two and three dimensions

## Slide 4: Spectrally Selective Field-Concentrating Optical Resonators Inspired by MMs
Narrow resonances (high-Q) + Strong field enhancements  Small changes of local environment can strongly affect optical response
Controlling optical response using minute amounts of material, e.g. atomic monolayer of graphene, protein monolayers
Ultra-sensitive fingerprinting/characterization of trace amounts of biological matter (protein monolayers, single cells, etc.)
Wu et. al. (Altug & Shvets), Nature Mat. 11, 69 (2012)
High-Precision graphene spectroscopy and ultrafast optoelectronic devices
Wu et. al. (Shvets), Nature Comm. (2014, in print)
IR Bio-Spectroscopy: from designing better immunosensors to single-cell fingerprinting

## Slide 5
Meta-Surfaces Based on Split Rings
Easy to turn “Fano”-resonant metasurfaces into active ones:
Strong field enhancement  small amounts of active material (e.g., graphene) is needed
Even small spectral shifts translate into large changes in transmission/reflection
One dark and one bright resonance
Continuum + 2 dark resonances
Notes: We are conducting now extensive theoretical/computational research aimed at understanding resonances of perforated films. Using several types of electromagnetic simulations (direct frequency scans of the field enhancement in response to imposed electric field, eigenvalue electromagnetic and electrostatic formulations, surface impedance method, direct electromagnetic simulations with incident light), we are zeroing in on several types of resonances. Some examples are shown in this slide, but this is still very much work in progress (stimulated by both existing and forthcoming experimental measurements: we have fabricated a number of perforated arrays of different hole diameter, spacing, and film thickness). In this slide I concentrate on the so-called even modes: the in-plane electric field is even with respect to the mid-plane of the film.Two types of resonances have been identified. One is the Localised Surface Polariton (LSP): the fields are tightly concentrated near the hole, and its frequency is independent of the periodicity. The other one is the Surface Phonon Polariton (SPP): the fields are very spread out, and SPP’s frequency is dependent on periodicity. Judging by the wavelength and the magnitude of the field enhancement, it appears that experimentally we’re exciting the SPP. However, we have not yet investigated the resonances which have the in-plane electric field ODD with respect to the mid-plane of the film. Such resonances have a non-vanishing magnetic moment – there is a hope for developing negative-epsilon, negative-mu surfaces!

## Slide 6: Outline of the Talk
Plasmonic Meta-Surfaces Functionalized with Graphene
The All-Dielectric Metasurfaces: Beating the Ohmic Loss
Emulating the electron spin in photons using metamaterials: Photonic Topological Insulators
Metamaterials-enhanced IR spectroscopy in life sciences: from proteins to cells
Metamaterials and metamaterials-inspired photonic structures are already contributing to investigating condensed and soft matter materials such as graphene, proteins, cells
They may soon contribute to emulating many-body interactions in condensed matter systems such as topological insulators
The most exciting future work is likely to be done at the meso-scale, e.g., “slightly” sub-wavelength, “somewhat” coherent MMs interacting with wavelength-scale objects (i.e. biological cells)

## Slide 7
Metasurface tuning using “lossless” SLG
MMs enable graphene characterization in mid-IR
SLG’s mid-IR response is weak: small Drude conductivity and no interband transitions, but…
Mid-IR Meta-Surfaces Enhance Graphene’s Response and Can be Controlled by SLG
Graphene is a low-loss plasmonic material in mid-infrared
. S. H. Mousavi et. al., Nano Letters 13, 1111 (2013).
Induction/Resistance

## Slide 8
Integration of MMs with Gated SLG
Back-gating injects carriers into graphene  shifts Fermi energy, changes conductivity
Graphene’s conductivity affects metamaterial’s resonances  graphene spectroscopy
Frequency shift comparable to linewidth  strongly-coupled regime of graphene-MM interaction
Voltage Vg
Holes
Electrons
Dirac Point
Silicon
SiO2
Graphene: free + bound carriers
Small (70nm) gap
Antenna arrays: N. K. Emani et. al., Nano Lett. 12, 5202 (2012); Y. Yao et. al., NanoLetters 13, 1257 (2013)

## Slide 9
Frequency and linewidth changes induced by graphene’s carriers
Calculate Fermi energy and carrier relaxation time in the Drude model of graphene conductivity
SRR Dipole
Monopole
Double-Fano Resonance Fit Used to Extract Graphene’s Optical Properties
Best fit:
Transport:

## Slide 10
Amplitude Modulator Based on MM/SLG
7dB modulation for
Modulation Depth
Modulation Depth
Modulate reflectivity around Dirac point by back-gating graphene
Monopole
Dipole
Modulation Depth:
Two properties satisfied by efficient modulators:
High baseline “on” reflectivity ()
High modulation depth (maximum )
Metamaterials + graphene have both

## Slide 11
IR Amplitude/Phase Modulator with SLG
Either phase or amplitude can be electrically modulated
Independently controlled pixels  electrically controllable IR beam steering or modulation or both
This can be done either in reflection or in transmission
Substrate
Spacer
Graphene
Meta pixel 1
Meta pixel 2
Meta pixel 3
Incident/Reflected IR Light
phase change
amplitude change

## Slide 12
C. Wu et. al., “Spectrally Selective Chiral Silicon Metasurfaces Based on Infrared Fano Resonances”, Nature Communications (in press, 2014)
All-Dielectric Fano-Resonant 2D Chiral Metasurfaces: Order of Magnitude Higher Q Than Similar Metallic Metasurfaces
Silicon
Metal
Cross-polarized transmission Txy

## Slide 13
High-Q Fano Resonance in Dielectric MSs
Free-space FTIR spectroscopy using low-NA (=0.14) normally incident IR beam focused to W=200mm
Experiment, Txy

## Slide 14
Collective Effects In Metasurfaces
Each unit cell interacts with 2-3 neighbors on each side horizontally and about 1 cell on each side vertically  short-range interaction
Pixels as small as have identical as infinite arrays
Pixels as small as 3 have  number of peripheral cells exceeds the number of central cells
Near-neighbor interactions are important in collective meta-surfaces, but not nearly as much as in 2D photonic crystals  distinct concept
A 2D PhC with operating at would have to be rather large (), and would require a collimated beam with
5x5 array
10x5 array

## Slide 15
Importance of Close-Neighbor Interactions
Near-field excitation reveals a narrow-band peak in the photonic density of states
Collective close-neighbor interactions persist over periods  each unit cell must have at least 2 nearest neighbors on each side horizontally
Conceptually different from PhC  “almost-collective” metasurface
Single-cell response: broad poorly expressed resonance

## Slide 16
LP CP: Stokes Parameter Extraction
RCP
Rotating analyzer Stokes polarimetry
LPCP conversion by 1 micron thick MS with high efficiency (50%) at normal incidence
Experimentally measured quality factor
Close to 100% Degree of Circular Polarization
How does LPCP conversion work?
How is it different from regular birefringence or 3D chiral structures?
Can one use chiral MS for developing a CP thermal emitter?
¼ wave plate
¼ wave plate
polarizer
=

## Slide 17: Super-Chiral Metasurfaces
Objective:  high Degree of Circular Polarization
and ,
Only RCP gets transmitted. And when it does, it gets flipped into LCP!
All of LCP gets reflected…as LCP Super-Chiral Mirror!
and ,
The effect does not require (a) dissipation, (b) substrate/air mismatch, (c) non-normal incidence  [¼ plate + polarizer + ¼plate] 1 thick!
It requires finite thickness ( impossible with noble metals), periodicity, and bi-anisotropy ()

## Slide 18
Spectrally Selective CP Thermal Emission
: more than 12 CP emission lines separated by 6- inside the IR transparency window
The entire scene emits thermal IR, but it is not circularly polarized  unique opportunities for IR Identification Tags
Each line can be RCP, LCP, or un-polarized: unique IR identification tags with unique spectral/polarization signatures
RCP/LCP Reflectivity Matrix
Reflectivity asymmetry  emissivity asymmetry
Infrared ID Tags Applications: Unique Spectral/Polarization Signatures!
Degree of Chiral Dichroism

## Slide 19: Avoiding Reflections Using Photonic Topological Protection
Property of a scalar wave equation: any obstacle/bend on the scale of one wavelength is going to cause reflections of the microwaves!
This is true for either bulk or surface waves
There is a precedent of suppressed reflections in physics: an electron with spin- ½ and strong spin-orbit coupling propagates without scattering!
A. Khanikaev et. al., Nature Materials 12, 233 (2013)

## Slide 20
Emulating Electron Spins and Topological Insulators Using Bi-anisotropic Metamaterials
A. Khanikaev et. al., Nature Materials 12, 233 (2013)
Bi-anisotropy requires breaking mirror reflection symmetry

## Slide 21: From Metamaterial to Meta-Crystal
Photonic equivalents of spin-up and spin-down electron states
Requires spin-degenerate metamaterials: =, =
Exact emulation of Kane-Mele Hamiltonian of graphene TIs
2-D PhMC: Photonic Crystal comprised of metamaterial inclusions
Bi-anisotropy parameters

## Slide 22: Interfaces: Edge States of PTIs
Interfaces between PTIs (e.g. between and ) support one-way spin-degenerate states!
LCP
RCP
“Spins” don’t scatter into each other as long as the materials are spin-degenerate: =, = restricted topological protection
Spin degree of freedom  relative phase between Ez and Hz
Orbital degree of freedom  CP at K point of Brillouin zone
Gap
Gap

## Slide 23: From Meta-Crystals to Meso-MMs
topologically protected surface waves
Topological Interface
RCP
LCP
RCP
LCP
32 units
20 units
Spin-polarized photon flow: two spin-up states moving forward, two spin-down states moving backward
Topological protection of edge states against backscatter
Fundamentally different from Tamm states!
Bi-anisotropic Meta-Waveguide (BMW)  simplified version of PTIs emulates spin-orbit coupling
Positive Index I:
Negative Index II

## Slide 24: Tamm States vs Topologically Protected Edge States: Disorder Sensitivity
32 units
20 units
“Cavity” placed along the interface  transmission depends on the nature of edge state:
Tamm state  small transmission interrupted by Fabry-Perot resonances
Topologically protected edge state  nearly perfect transmission  guide waves around corners
“Robust” topologically protected edge state:
“Fragile” Tamm surface state:
FP resonances
Topological protection
Non-trivial interface

## Slide 25: Breaking topological protection
chiral edge mode
Gapless rods
Off resonance
Cavity eigenmode couples spin states  resonant backscattering is allowed by spin-flipping!
Two-mode theory collapses in the presence of third mode!
Nonlinearities also break topological protection  emulation of many-body effects in CM
Resonant magnetic impurity inside topological bandgap
PTI Interface
Off resonance
On resonance
Q-factor = 7500

## Slide 26: What Can Metamaterials Do For You: Applications Time!!
All-dielectric super-chiral metasurfaces with Q>100
C. Wu et.al., Nature Materials 11, 69 (2012)  surface-enhanced IR spectroscopy of protein monolayer; microfluidic integration for cell identification in blood (CTCs)
C. Wu et.al., Nature Comm. (in press)  engineering of thermal/quantum emission  sources of CP radiation across EM spectrum
S. H. Mousavi et. al., NL 13, 1111 (2013)  integration of SLG with metamaterials  agile IR modulators, beam steering.

## Slide 27: Acknowledgements
Postdocs/Staff:
Simeon Trendafilov
PhD Students
S. Austin Yi Nihal Arju Hossein Moussavi Nima Dabidian Chih-Hui Wu
Collaborators:
Igal Brener (SNL) Rod Ruoff (UT)

## Slide 28: Additional Slides

## Slide 29
Novel platform for bio-sensing and molecular fingerprinting: Metasurface Enhanced Infrared Reflection Spectroscopy  MEIRS
Objective: better biosensor by improving the orientation of binding proteins and antibodies  higher binding capacity
substrate
Chihhui Wu et.al., Nature Materials 11, 69 (2012)
Notes: A standard biosensor (or immunoassay) works by immobilizing antibodies on a solid substrate and detecting its binding with antigens of interest (anything from cells to proteins). Only one region of an antibody binds to an antigen. Therefore, it is important that the antibody presents itself to an antigen in the right orientation. This can be done by using intemediate binding proteins that bind to a specific (Fc) portion of an antibody. However, there is no direct evidence that the binding proteins themselves properly orient themselves. So far antibody orientation has been deduced from immunological activity of immobilized antibodies. This method is indirect!

## Slide 30: Meta-Pixels Mosaic Tuned to Fingerprints
Pixels’ resonance frequencies can be swept across vibrational resonances
Resonant and non-resonant pixels  additional data points for bio-sensing
Size determines natural frequency
50 elements
Notes: We can make mosaics of meta-pixels tuned to different vibrational resonances

## Slide 31
How sensitive is MEIRS: Comparison with Fluorescence Measurements
Single monolayers of fluorescently tagged antibodies are difficult to detect using unspecialized microscopes
Metasurface-enhanced infrared spectroscopy (MEIRS) enables the detection of antibody monolayers  strongest signal when metasurface resonance is matched to vibrational resonance of the protein (e.g., Amide I)
Advantageous to avoid exogenous labels for tagging
Fluorescently tagged antibodies before washing
Attached antibodies (after washing): fluorescence not observed under microscope
Attached antibodies
Amide I
: Difference spectrum (with protein – bare)  peaks at the MM resonance
Notes: We are conducting now extensive theoretical/computational research aimed at understanding resonances of perforated films. Using several types of electromagnetic simulations (direct frequency scans of the field enhancement in response to imposed electric field, eigenvalue electromagnetic and electrostatic formulations, surface impedance method, direct electromagnetic simulations with incident light), we are zeroing in on several types of resonances. Some examples are shown in this slide, but this is still very much work in progress (stimulated by both existing and forthcoming experimental measurements: we have fabricated a number of perforated arrays of different hole diameter, spacing, and film thickness). In this slide I concentrate on the so-called even modes: the in-plane electric field is even with respect to the mid-plane of the film.Two types of resonances have been identified. One is the Localised Surface Polariton (LSP): the fields are tightly concentrated near the hole, and its frequency is independent of the periodicity. The other one is the Surface Phonon Polariton (SPP): the fields are very spread out, and SPP’s frequency is dependent on periodicity. Judging by the wavelength and the magnitude of the field enhancement, it appears that experimentally we’re exciting the SPP. However, we have not yet investigated the resonances which have the in-plane electric field ODD with respect to the mid-plane of the film. Such resonances have a non-vanishing magnetic moment – there is a hope for developing negative-epsilon, negative-mu surfaces!

## Slide 32: Interaction of Anisotropic and Oriented Proteins with Metasurfaces
orientation tensor: C=O bond with respect to Cartesian axes
z
x
qz
qx
Orientation of anisotropic proteins detected by surface-enhanced spectroscopy
From Protein Data Base
Isotropic IgG protein
Anisotropic protein A/G
for isotropic proteins
Notes: As it turns out, many proteins are not really isotropic. They are more like pasta: very elongated in one direction. This can be described by the so-called
directional tensor T. For an isotropic protein this tensor is a unity matrix. What about real proteins?

## Slide 33: MEIRS determines protein layer compositions
Binding of A/G monolayer of thickness h1=2.7nm to three FRAMM pixels (blue, green, red)
Non-resonant blue pixel is not vibration sensitive SPR-like thickness measurement
Resonant green pixel is vibration/orientation sensitive  orientation of A/G on the surface
mono-layer: dash
Differential Reflectivity
C. Wu et.al., Nature Materials 11, 69 (2012)

## Slide 34: MEIRS determine protein layer compositions
IgG monolayer of height h2 = 5.1nm binds to A/G monolayer of height h1=2.7nm  (h2 + h1)/h1 = 2.9
Non-resonant blue pixel is not vibration sensitive SPR-like thickness measurement
Resonant green pixel is vibration/orientation sensitive  orientation of A/G on the surface
mono-layer: dash bi-layer: solid
Differential Reflectivity

## Slide 35: Where do we go from here: From Proteins to Cells to Diagnostics
glycogen (1020 cm-1)
phosphate (1080 cm-1)
Spectral signatures of cancer cells
C. Wu et.al., Nature Materials 11, 69 (2012)
Notes: Advantage of metamaterials: high field localization (tens of nm) which is comparable with the total thickness of binding antibodies and cellular membrane proteins. Also: this sensor has a large dynamic range, i.e. it enables monitoring protein binding, cell attachment, etc.

## Slide 36: Metamaterials-Based Fingerprinting of Live Cells: Macrophages vs Malignant
Epithelial cancer cells
Normal macrophage cells
glycogen (1080 cm-1)
phosphate (1030 cm-1)
C=O ester in P-lipids
Amide I
Amide II
DNA/RNA (P=O)
Future: detection and identification of circulating tumor cells (CTCs): the key cause of cancer-related mortality because of metastasis
Notes: Advantage of metamaterials: high field localization (tens of nm) which is comparable with the total thickness of binding antibodies and cellular membrane proteins. Also: this sensor has a large dynamic range, i.e. it enables monitoring protein binding, cell attachment, etc.