## Slide 1
van der Waals Heterostructures: Fabrication and Materials Issues
J. Hone
Columbia University
Mechanical Engineering
Center for Precision Assembly of Superstratic and Superatomic Solids (PAS3) – Columbia / CCNY MRSEC

## Slide 2
Novoselov, Geim, Science (2005), Nature (2005); Zhang, Kim, Nat. (2005)
Graphene on SiO2
Field effect mobility
mobility ~20,000 cm2/Vs
surface roughness
scattering from charged impurities
disorder from charged impurities
Martin, et al, Nature Phys. (2008)
Graphene on SiO2:

## Slide 3
Boron Nitride
 | Band Gap | Dielectric Constant | Optical Phonon Energy
BN | 5.8 eV | ~3.5 | >100 meV
SiO2 | 8.9 eV | 3.9 | 59 meV
Optical properties of h-BN
< 2% lattice mismatch to graphene
atomically flat
chemically inert, stable to high temp.
no dangling bonds
good dielectric properties
Boron Nitride – graphene’s insulating ‘cousin’

## Slide 4
Watanabe, K., Taniguchi, T. & Kanda, H. “Direct-bandgap properties and evidence for ultraviolet lasing of hexagonal boron nitride single crystal.” Nature Mater. 3, 404–409 (2004).
Taniguchi, T. & Watanabe, K. “Synthesis of high-purity boron nitride single
crystals under high pressure by using Ba–Bn solvent.” J. Cryst. Growth 303, 525–529 (2007).
The Source…

## Slide 5
C.R. Dean, A.F. Young, I. Meric, C. Lee, L. Wang, S.Sorgenfrei,
K. Watanabe, T. Taniguchi, P. Kim, K.L. Shepard, J. Hone, Nature Nano (2010)
‘Polymer transfer’ of graphene onto BN

## Slide 6
Improved Performance
Enhanced mobility
lower disorder
Many FQHE states

## Slide 7
Making Layered Structures
The vision….
Geim, Nature 2013

## Slide 8
BN
G
10 µm
Making Layered Structures
The reality…
BN
Graphene

## Slide 9
BN
G
BN
G
BN
10 µm
Making Layered Structures
The reality…
BN
Graphene

## Slide 10
BN
G
BN
G
BN
10 µm
Making Layered Structures
The reality…
BN
Graphene
polymer residue

## Slide 11
Van der Waals Assembly
L. Wang et al, Science (2013)
Ultraclean technique – graphene never exposed to polymer

## Slide 12
Side Contacts

## Slide 13
Achieving ideal electrical performance
Sheet resistance below 40 Ω – more conductive than silver or copper!
At limit of acoustic phonon scattering.
Highest R.T. mobility of any material!

## Slide 14
Low-T Ballistic Transport
Transport is ballistic at low T up to at least ~15 µm

## Slide 15
Ultra-clean graphene: magneto-transport
’Hofstader Butterfly’
Negative Refraction
Exciton Condensation

## Slide 16
graphene – BN moire’ pattern
For well-aligned structure, a ~ 15 nm
a
Hofstader, PRB 1976:
Basic problem: What are Bloch states in 2D with lattice + magnetic field? (2 length scales)
Energy bands develop fractal structure when magnetic length is of order the periodic unit cell
Wannier (1977): Fractal gaps trace out straight lines in n vs. flux, with two quantum numbers (s,t)
Hofstadter’s Butterfly

## Slide 17
1st generation: polymer transfer
C. R. Dean, L. Wang, …, JH, P. Kim, Nature (2013)
n (cm-2)
B (T)
Rxx
Also: Ponomarenko, Novoselov, Geim (Nature);
Hunt, Jarillo-Herrero (Science)

## Slide 18
2nd generation – van der Waals assembly
L. Wang, JH, C. Dean, in preparation

## Slide 19
States within Hofstader spectrum
fractional quantum Hall states
Fractal states
New states
Fractal states: integer t, s
FQHE: fractional t
New states: fractional s
Wang, L., Gao, Y., Wen, B., Han, Z., Taniguchi, T., Watanabe, K., Koshino, M., Hone, J. & Dean, C. R. Science 350, 1231-1234, (2015).

## Slide 20: Using Magnetic Focusing to Study Refraction
S. Chen… JH, A. Ghosh, C. Dean, Science (2017)

## Slide 21: Negative refraction in p-n junctions
Simple geometric model fits shape of focusing peaks
Positive and negative Snell’s law confirmed
Experiment

## Slide 22
Exciton Condensation in Bilayer Graphene Superlattices
J. Li, JH, C. Dean, under review (Nature). Also P. Kim group
Counterflow
B
Parallel Flow
Coulomb Hall drag

## Slide 23: Evidence for Condensate phase at 𝜈tot = 1
At vT = 1, drive and drag layer both show quantized Hall resistance
In counterflow geometry, Hall drag = 0 at vT = 1

## Slide 24
New Control of Graphene Devices
Artificial Superlattices
Gate-defined structures
Interlayer Rotation

## Slide 25
Triangular lattice of holes in SiO2, 40nm periodicity
Artificial Superlattices

## Slide 26
How can we make graphene even better?
Use graphite as top / bottom gates: better electrostatic uniformity
Use top gate to define channel region
Adjust back gate / Magnetic field to maintain insulating (v=0) state
Notes: This new generation of graphene devices takes advantage of the properties of graphene under a high magnetic field to define electrostatically new structures, in this case Hall bars (a). The main idea of these devices is to avoid edge disorder and electrostatic variations in the device due to fringe field.
In a high enough magnetic field (normally around 4 T) the nu= 0 state of graphene opens an energy gap, which has the particularity of not having edge states. Our double gated devices have a global back gate which sets the fermi energy of the external part of the device in this nu=0 gap while the top gate is used to tune the Fermi energy of the Hall bar (b). Our devices also have current leads that are not covered by the top gate to assure that the external part of the top gate is in an insulating state (d). Using these uncovered leads we can see that the insulating state is present from 4 T for the whole gate range.

## Slide 27
Gate defined - metal
Etched
Gate defined - graphite
Qualitative Improvement in QHE
Notes: Here we have the results for three differnet type of devices: dual gated, where the gates cover the whole device, gate defined –metal where the top gate is smaller than the back gate as described before and gate defined – graphite where the top gate is also smaller but this time made of graphite. We can see that the effects of the gate defined are striking, at moderated magnetic field (15 T) the dual gated device do not show any hint of fractional quantum Hall effect in the N=1 LL while the both gate defined devices do.
Maybe the more remarkable characteristic is that the gate defined- graphite shows a higher quality with moch more fractional states developing at the same magnetic field. Nevertheless, as demonstrated in GaAs samples, the quality of the device is so good that the plateaus of the FQH become very small, this is explained by a small amount of scattering centers which makes localization very hard to achieve.

## Slide 28
New physics reachable thanks to the gate defined devices
Reentrance state
Notes: Desides the observation of FHQ effects at lower magnetic fields and the and the new information this brings about how disorder is affecting the quantum Hall effect in graphene these new structures also new physics, not observed before in transport measurements, is not reachable. Amount them the observation of the four-flux states FQHE and the observation of reentrance of the integer quantum Hall effect with a very particular symmetry which could be associated with to the symmetries of the LL.

## Slide 29
New physics reachable thanks to the gate defined devices
Re-entrant quantum Hall states
Notes: Desides the observation of FHQ effects at lower magnetic fields and the and the new information this brings about how disorder is affecting the quantum Hall effect in graphene these new structures also new physics, not observed before in transport measurements, is not reachable. Amount them the observation of the four-flux states FQHE and the observation of reentrance of the integer quantum Hall effect with a very particular symmetry which could be associated with to the symmetries of the LL.

## Slide 30
Controlling Interlayer Rotation
Chari, Ribero, Dean, Shepard, Nano Lett (2016)
Angle-dependent contact resistance between graphene and graphite
Notes: In situ manipulation of the electronic band structure of graphene by a Moiré supperlattice is now possible. This is achieved using a set of new devices consisting of (from bottom to top) a graphite gate, h-BN, graphene and a smaller prechasped h-BN piece. The Moiré periodic potential will appear due to the difference in lattice constant of graphene and BN, when these two are close to alignment. In here we manipulate in situ the crystallographic orientation of BN and graphene using an AFM tip in contact mode. The advantage of this technique is not only that it allows to control the angle between two materials but it permit to measure the electrical properties as the angle is changed, creating a technique to really investigate the effects of crystallographic orientations between 2D materials as a function of the angle.

## Slide 31
BN on graphene (band structure manipulation)
BN
graphene
BN handle
Contacts
Graphite gate
AFM tip
HSQ/BN
Controlling Interlayer Rotation: Graphene / BN
Shape ‘handle’ structure
Rotate with AFM
Measure transport
Notes: In situ manipulation of the electronic band structure of graphene by a Moiré supperlattice is now possible. This is achieved using a set of new devices consisting of (from bottom to top) a graphite gate, h-BN, graphene and a smaller prechasped h-BN piece. The Moiré periodic potential will appear due to the difference in lattice constant of graphene and BN, when these two are close to alignment. In here we manipulate in situ the crystallographic orientation of BN and graphene using an AFM tip in contact mode. The advantage of this technique is not only that it allows to control the angle between two materials but it permit to measure the electrical properties as the angle is changed, creating a technique to really investigate the effects of crystallographic orientations between 2D materials as a function of the angle.

## Slide 32
BN on graphene (friction)
photodiode
Graphite/BN
Interlayer friction
Layers ‘lock’ together at commensurate angles
Notes: Once the devices are build we use friction measurements between the two materials to pre-align them. We found out that in fact the friction response between graphene and BN is neglictible over a wide range of angle except when these two materials are aligned one to the other.

## Slide 33
BN on graphene (band structure manipulation)
l=14 nm
l=10 nm
l
Controlling Moire’ Wavelength
Notes: If we measure the transport response as a function of the angle we find the expected appearance of the satellite peak due to the band structure modification by the Moiré potential. This peak can be mapped out for a wide range of angles which corresponds with a variation of the Moiré length from 14 nm to 10 nm.

## Slide 34
Graphene Light Sources
Suspended Graphene Emitters
Ultrafast BN-encapsulated Emitters

## Slide 35
2D Semiconductors

## Slide 36
Encapsulated MoS2 with graphene contacts
X. Cui, G. H. Lee et al.,Nature Nano (2015)

## Slide 37
Multi-terminal transport
Electron-phonon mobility: µ~T-2 for all samples
contrast to on SiO2
Independent of gate voltage
50-150 at R.T.
Hall mobility

## Slide 38
Quantum Oscillations
Tunable SdH Oscillations in monolayer MoS2
B (T)
VBG (V)
Rxx (kΩ)

## Slide 39
2D Semiconductors – current challenges
Contacts
Achieiving intrinsic optical properties
Materials Quality

## Slide 40
Contacts to TMDCs
A. Allain. Nature Mat. (2015)
Metal contacts: Fermi Level Pinning maintains Schottky barrier even with large change in metal work function
Can make Ohmic contacts with graphene – but only at very high carrier density for monlayers

## Slide 41
Hybrid Metal / hBN Contacts
Theory: strong hybridization between transition metals and hBN/graphene strongly shifts work function
(M. Farmanbar et al. PRB. (2016))

## Slide 42
Approaching the Intrinsic Limit for TMD PL
G. Moody, …., A. Knorr, X. Li, Nat. Comm 2015
2DFTS measurements:
Extrinsic
broadening: > 10 meV
Intrinsic
broadening: ~ 2 meV
Can we minimize or eliminate extrinsic effects?
WSe2

## Slide 43
Approaching the Intrinsic Limit for TMD PL
T = 4 K
O. Ajayi, T. Heinz, S. Strauf, XY Zhu, JH, submitted

## Slide 44
Approaching the Intrinsic Limit for TMD PL
Highly consistent spectra
Broad low-E absorption
High-E ’shoulder’

## Slide 45
Approaching the Intrinsic Limit for TMD PL
FWHM ~ 2 meV
Voigt Fit (Lorentzian with Gaussian broadening)
Homogeneous width ~ 1.4 meV
Heterogeneous brodening ~ 0.9 meV

## Slide 46
          100nm
          100nm
2.6% of Mo are vacancies
1.28 % Interstitial or Antisites per Mo
.33% of Mo are vacancies
.16 % Interstitial or Antisites per Mo
Atomic defects in TMDs
Commercial MoSe2
Home-grown MoSe2
Growth: Hone / Barmak groups STM imaging: Pasupathy group

## Slide 47
Atomic defects in TMDs
Most common defects are metal vacancies or interstitials

## Slide 48
How can we get better?
Commercial MoSe2
Home-grown MoSe2
77 K
PL yield dominated by point defects (Mo and Se vacancies)

## Slide 49
CDW (1T-TaS2, TaSe2,
VSe2, TiSe2)
SDW
(FeTe)
SC
(FeSe)
FeTeS, FeTeSe
2H-TaS2, TaSe2, NbSe2
Air-sensitive 2D Materials
FeSe
FeTe
FeSexTe1-x
Air-sensitive materials
Novel Phenomena

## Slide 50: Incandescent Visible Light Emission
Unpublished
Stable emission for ~ 10 minutes in air
Stable emission for ~ 10 years in vacuum

## Slide 51: 2D ‘Stacking’ system in glovebox
Encapsulate in glove box using hBN
Fabricate electrodes etc. afterward

## Slide 52
Staley, PRB 2009
Superconductivity in 2D NbSe2
Prior work:
Bulk superconducting with Tc ~ 5 K
Thin NbSe2 is not superconducting
High sheet resistance (disordered limit?)

## Slide 53
Superconductivity in BN-encapsulated bilayer NbSe2
2-layer NbSe2
AW Tsen, B Hunt, YD Kim, ZJ Yuan, S Jia, RJ Cava, J Hone, P Kim, CR Dean, AN Pasupathy, Nature Physics (2016)

## Slide 54
Scaleup – CVD-grown hBN
S. Kim… YH Lee, J. Kong, Nat. Comm (2015)

## Slide 55
Scaleup – passivating SiO2
Si
SiO2
BN
SAM
Graphene
C. Zhang, XY Zhu, JH, unpublished

## Slide 56: Major Contributors
Hone group:
Y-D Kim
Lei Wang
Yuanda Gao
Alex Cui
Ghidewon Arefe
Demi Ajayi
Jenny Ardelean
Julia Zhang
Funding: NSF MRSEC, NSF DMR, SRC / INDEX, DOE BES, ONR, AFOSR BRI
Pasupathy group
Drew Edelberg
Kim group (Harvard)
S. Strauf group (Stevens Inst.)
T. Taniguchi, K. Watanabe (NIMS, Japan)
Dean group:
Rebeca Ribeiro
Shaowen Chen
Jia Li
En-min Shih