## Slide 1: Plasma-Materials and Divertor Options for Fusion
Presented to:
National Academy of Sciences Panel
A Strategic Plan for U.S. Burning Plasma Research
J. Rapp

## Slide 2: Lifetime of divertor will deterimine fusion reactor availability
Main driver of scheduled maintenance: divertor (and blanket)
Coolant manifold
(permanent)
TF coils
Upper ports
(modules and coolant)
Blanket modules
5-6 yrs lifetime
Divertor plates
2 yrs lifetime goal
Cool shield
30cm
(permanent)
Lower ports
(divertor)
Central ports
(modules)
Vacuum vessel
70cm
(permanent)
Cost of electricity is proportional to (1/A)0.6

## Slide 3: Outline
Plasma-Material Interaction (PMI) challenges
Potential Plasma-Facing Materials (PFMs) and Components (PFCs)
Current status of U.S. PMI research
Facilities needed for the development of PFCs
Strategic elements to accelerate U.S. burning plasma research
A proposed high-level R&D program and roadmap for PMI

## Slide 4: Outline
Plasma-Material Interaction (PMI) challenges
Potential Plasma-Facing Materials (PFMs) and Components (PFCs)
Current status of U.S. PMI research
Facilities needed for the development of PFCs
Strategic elements to accelerate U.S. burning plasma research
A proposed high-level R&D program and roadmap for PMI

## Slide 5: Challenges for materials: fluxes and fluence, temperatures
JET ITER FNSF Fusion Reactor
50 x divertor ion fluxes
up to 100 x neutron fluence (150dpa)
5000 x divertor ion fluence
106 x neutron fluence (1dpa)
up to 5 x ion fluence
P/R about the same
5-10 x P/R

## Slide 6: Plasma Material Interactions (PMI) in fusion reactor
Erosion
(chemical and physical)
Ablation
Melting (metals)
Re-deposition
Co-deposition of
hydrogen
Implantation
Strongly Coupled regime:
Eroded material is trapped in plasma (highly collisional) near target, and re-deposited on surface due to incoming flows, electro-static acceleration and motion in magnetic field
Long exposure to damaging plasma flux  thick layers of re-deposited material
Every surface atom is displaced ~ 107 times in a divertor lifetime
Material in a reactor divertor is NOT what was installed, we need a way to create and test plasma-reformed surfaces
carbon target
Worst case erosion rate ~ m/yr !

## Slide 7
StSt (TEXT, PLT), Mo (Alcator-A, TFR), W (DOUBLET-II, ORMAK), Al (ST), Al2O3 (PETULA), B4C (TFR), Be (ISX-B, JET), Au (DIVA), Ti (PDX, DITE), Li (CDX-U), TiC (W-AS), TiB2 (ISX-B), Cu (ASDEX), C (CFC, graphite)…
Quite some materials have been tested as PFM over the years:
PLT used a carbon limiter 50% increase in Te
Following those results, C (graphite, CFC) became the material choice for most devices
Only recently the interest in high-Z PFCs is growing again, mainly because of the observed Tritium retention during TFTR and JET DT experiments.
Plasma Surface Interactions
Challenge: material choice for PFCs

## Slide 8: ITER, material choice
Beryllium
Tungsten
Carbon, now Tungsten
Be low radiation
C non-melting CFC
W high melting point, low erosion by D, T

## Slide 9: Power exhaust challenge
Issues
A significant part of the radiation is not in the SOL, PSOL/R ~ 7 has been achieved on AUG so far (ITER: PSOL/R ~ 12)
High P/R for DEMO is challenge
High Pheat/PLH does allow for significant core radiation in DEMO, ARIES-ACT1 (frad, core~ 70 - 80%); AUG has demonstrated 70% core radiation without loss of confinement
PSOL B / R could be reduced to 100-200
Kallenbach, NF 2009
Rapp, DEMO workshop 2011
Kallenbach, NF 52 (2012) 122003
C Kessel et al., FST 2015
D Maisonnier et al., FED 2006
 | PPCS A | ARIES-ACT1 | ITER | JET | AUG
Pheat/R [MW/m] | 130 | 65 | 19.8 | 11.4 | 14
f*rad wo br, syn rad | 0.64 | 0.67 | 0.54 | 0.76 | 0.87
P*heat B/R [MW T/m] | 651 | 306 | 80 | 39 | 35
PLH B/R [MW T/m] | 202 | 105 |  |  | 
bN | 3.5 | 4.75 | 1.77 | 1.6 | 3

## Slide 10: Power exhaust with impurity seeding: what about confinement?
H98(y,2) has been found to be bN dependent
Impurities can improve confinement
Despite bN scaling and impurity effect on core confinement, it is uncertain if high H98(y,2) of 1.2 or 1.6 can be reached with strongly radiating mantle and plasma core
H98(y,2)
H98(y,2)
bN
bN
A. Huber, EPS 2014
M. Wischmeier, IAEA 2014
J. Rapp, Nucl. Fusion 52, 2012, 122002
AUG
JET

## Slide 11: Power exhaust: advanced divertors
If radiative dissipation of power is not sufficient, advanced divertors might help.
Courtesy, B. LaBombard

## Slide 12: Challenges for materials: fluxes and fluence, temperatures
JET ITER Fusion DEMO
50 x divertor ion fluxes
up to 100 x neutron fluence (150dpa)
5000 x divertor ion fluence
106 x neutron fluence (1dpa)
up to 5 x ion fluence
Materials need to be developed and tested under fusion prototypic conditions:
High fluxes, high ion fluence, high neutron fluence
PSOL B/R about the same
3 x PSOL B/R

## Slide 13: Reactor: high plasma performance and high PFC lifetime requires strong re-deposition to ensure low net erosion
Divertor plasma temperature in the ~ 10 eV range where GROSS sputtering yield of tungsten drops to ~ 10 X greater than the required NET sputtering yield.
Reactor divertor lifetime ~108 s requires net erosion rate of 10-6
~ 100 X required net yield
~ 10 X
~ 1 X
net
erosion
erosion
net
deposition
DX
Main chamber erosion due to ions and high energy CX neutrals (ITER: ECX ~ 500 eV; DEMO = ??)
If re-deposition of W at main chamber is not increased, massive amounts of W migrate to divertor (t/yr) Behrisch J. Nucl. Mater 313 (2003) 388
How does W surface evolve with strong deposition of W?
Grain size, crystal structure, dust?
Krieger J. Nucl. Mater 266 (1999) 207

## Slide 14: High fluence and frequent ELMs might change W erosion processes
T Loewenhoff et al., Nucl. Fusion 55 (2015) 123004
M Tokitani et al., Nucl. Fusion 51 (2011) 102001
MJ Baldwin et al., Nucl. Fusion 48 (2008) 035001
S Lindig et al., Phys. Scr. T145 (2011) 014039
Tungsten
100000 pulses
@ 0.3 MJ/m2
Tungsten
Tungsten
Y Ueda et al., Fus. Sci. Technol. 52 (2007) 513
Tungsten
Tungsten
Unipolar arcing, can possibly create W dust of nm size
High energy density plasma changes:
Surface area; Surface roughness
Surface potential (unipolar arcing may occur)
Surface temperature (loosely bound layers, He bubbles)
Surface chemical activity
Consequences:
Chemical and physical erosion yield
Relation between gross erosion and net erosion
Dust production might occur due to macroscopic erosion of surface structure and meltlayer splashing
Whole grain ejection can cause macroscopic erosion
M Wirtz et al., J. Nucl. Mater. 420 (2012) 218
J Coenen et al., Nucl. Fusion 51 (2011) 083008
Meltlayer splashing creates W dust of mm size
Neutron irradiation will likely enhance macroscopic erosion

## Slide 15: Tritium retention
Projected T-retention in ITER
Issues
Fluence dependence
Flux dependence
Effect of surface temperature
Effect of impurities (He, N, Ne, Ar) on T-transport in W
Neutron irradiation effects
Fluence dependence D retention in W
J Roth et al., J. Nucl. Mater. 390 (2009) 1
R Doerner et al., Nucl. Mater. Energy (2016)

## Slide 16: Neutron irradiation will influence PMI
Accumulation of He can have major implications for the integrity of plasma-facing- and structural-components
Neutron irradiation damage | Consequences on PMI
Thermal conductivity | Temperature operation window, less tolerance to transient heat loads, erosion yield
Chemical composition (transmutation) | Hydrogen retention, thermal conductivity indirectly
Interstitials, vacancies, dislocations, voids | Hydrogen retention
Swelling and irradiation creep at intermediate temperatures | Tolerance in PFC alignment will become larger, hence power handling capability lower
Loss of high-temperature creep strength | Reduced temperature operation window
Ductile to Brittle Transition Temperature | Reduced temperature operation window
He, H embrittlement | Erosion and dust production will be enhanced
Synergies of micro-structural changes between neutron and plasma irradiation | Increased erosion due to increased surface roughness
Grain boundary
Voids in F82H
9dpa, 380 appm He
Neutron irradiation will weaken grain boundaries and possibly leading to increased macroscopic erosion
14 MeV, high He/dpa
up to 150 dpa for blankets
up to 50 dpa for divertor

## Slide 17: T-retention in refractory metals and impact of irradiation
Most studies today rely on high energy ion irradiation (self implantation)
  Time scales of dpa creation are vastly different in those experiments
  Self implantation leads to shallow damaging zones
Some studies with HFIR irradiations started (up to 0.3 dpa)
  Plasma exposure is limited to low fluxes and low fluence
Deuterium retention is higher for irradiated tungsten
Deuterium retention is lower in mixed D-He plasmas
Suggests changed transport of D in the presence of He
Suggest the need to test neutron irradiated samples at high dpa (>> 0.3 dpa)
Investigation of neutron irradiated materials with relevant He/dpa ratio is required
Lipschultz, ITPA DivSOL 2010; HFIR: M. Shimada, et al., Nucl. Fusion 2015
HFIR irradiations
Alimov, J. Nucl.Mater. 420 (2012) 370 and other similar:
M. Baldwin et al, Nucl. Fusion (2011)
W. R. Wampler et al, Nucl. Fusion (2009)
dpa
He

## Slide 18: Ion irradiations important (but do not simulate neutrons)
Xu et al.,Acta Mater., 2015
W-2%Re
33 dpa ions 500°C
(Atom probe atom map)
P. Edmondson, ORNL
Pure W (99.9+%)
2.2 dpa HFIR 750°C
Now 5%Re-7%Os bulk
-phase interconnected ribbons
(Atom probe isodensity surface)
(Same scale)
How will tritium, helium, heat, etc., permeate this structure?
Notes: Chad:
“Because of irradiation. Ion irradiation is the best tool, the only tool, we have for rapid-screening experiments, for single variable experiments, for mechanistic explorations. But what it can’t do, is simulate neutron irradiation. At least not without a lot more back-and-forth than we’ve done on these materials so far. Did anyone expect a tapeworm morphology of interconnected sigma-phase at two dpa?”

## Slide 19: Could neutron irradiation lead to higher physical sputtering?
plasma irradiated  + plasma
27 dpa by 4 MeV He
Irradiation border
0 250 500 750
4
2
0
-2
-4
h [m]
L [m]
He ion irradiation has shown to change micro-structure in tungsten significantly (very high He/dpa, factor 100 too high).
Grazing incidence of plasma could lead to enhanced physical sputtering of roughened surface.
What is expected with neutron irradiation at relevant He/dpa ratio?
V.S. Koidan et al., IAEA 2010

## Slide 20: Challenges of free-flowing liquid metal PFCs
Fast flowing system: Kelvin-Helmholtz and Rayleigh-Taylor instabilities
Slow flowing system: high temperature -> evaporation
Surface composition change due to impurities
Tritium retention due to gettering by oxygen (Li)
Helium pumping
Vapor shielding
Thinning of liquid metal layer
Irradiation damage of substrate material
Corrosion
M Jaworski et al., PSI 2016, Nucl. Mater. Energy (2016)

## Slide 21: Outline
Plasma-Material Interaction (PMI) challenges
Potential Plasma-Facing Materials (PFMs) and Components (PFCs)
Current status of U.S. PMI research
Facilities needed for the development of PFCs
Strategic elements to accelerate U.S. burning plasma research
A proposed high-level R&D program and roadmap for PMI

## Slide 22: Development of materials for PFCs
Mechanically alloyed tungsten
Laminates
Fiber-reinforced composite materials
Self-passivating tungsten, “smart”, alloys
Functionally graded materials for fusion
Alternatives: ceramics
J.W. Coenen et al., Fus. Eng. Des. 1244 (2017) 964
A. Litnovsky et al., Phys. Scripta T170 (2017)
Ch. Linsmeier et al., Nucl. Fusion. 57 (2017) 092007
Ch. Linsmeier et al., Nucl. Fusion. 57 (2017) 092007

## Slide 23: Novel composite materials: Wf/W
Tungsten fibre
W-matrix
Pseudo-ductile behavior of tungsten fiber reinforced tungsten
Properties rely on energy dissipation mechanisms
Fiber pullout
Crack bridging
Crack deflection
Pure W fiber might not retain strength under irradiation
Can we modify fibers accordingly?
J.W. Coenen et al., Fus. Eng. Des. 1244 (2017) 964
J. Riesch et al., Report Max-Planck-IPP (2013)

## Slide 24: Exploring ceramics as PFM option
Material Properties | Pure Tungsten | Carbide CVD SiC | Isotope-separated Diborides |  | MAX Ti3SiC2
 |  |  | Zr11B2 | Ti11B2 | 
Atomic Number | High | Low | Medium | Medium | Medium
Melting Point (°C) | 3,422 | 2,730 | 3245 | 3225 | ~3,000
Max. Operating Temperature (°C) | ~ 1,100 | ~1,400 (?) | Unknown | Unknown | ~ 1,000 (?)
Thermal Cond. (W/m-K) Unirr - RT/1000°C Irradiated Degradation | 180/110 Moderate | 400/80 Harsh but with NFB* | 120/100 Unknown | 96/78 Unknown | 40/50 Small
Radiation Tolerance | Poor(?) | Good | Unknown | Unknown | Fair(?)
Tritium Permeability | Medium | Low | Unknown | Unknown | Unknown
Tritium Retention | Low | High? | Unknown | Unknown | Unknown
Neutron Absorption | High | Low | Low | Low | Medium
Short-term Activation | High | Low | Medium | Medium | Medium
Long-term Activation | Low | Low | Medium | Medium | Medium
LOCA Safety | Poor | Good | Fair(?) | Fair(?) | Good

## Slide 25: Advanced Materials enabled by new transformative technologies
Additive Manufacturing
Materials-by-Design driven by
Artificial Intelligence
Diffusion barriers,
Permeation barriers
Self-healing materials
High heat transfer technologies
Self-passivating
materials
Functionally graded materials
In-situ repair of PFCs

## Slide 26: Transformative enabling technology
What is the effect of innovation?
Higher heat fluxes
Larger temperature operation window
Larger stress resilience
Better compatibility with plasma
Better accident tolerance
Diffusion barriers / permeation barriers to lower tritium retention
Defect barriers to improve irradiation resistance
What to expect in the future from innovation?
Smaller
Faster
More complex
More precise
Example for current limitation:
Atom Layer Deposition (2D-layer) possible at low speed
3D-structures possible with Additive Manufacturing as small as 50mm
Materials-by-design on a micro- or nano-structure level to enable
bulk/surface PFC properties in complex geometries in a single graded system

## Slide 27: Complex heat transfer systems will be benefit from additive manufacturing
Microjets might open opportunity for power exhaust of up to 30 MW/m2
200 mm jets
W faceplate
Outlet plenum
W jetbody
Inlet plenum
Advanced manufacturing
Required!
q//
Temperature
HTC
Micro
116 jets
HEMJ
D Youchison, FST (2014)

## Slide 28: Opportunities for emerging materials
Design of radiation-resistant and radiation tolerant materials enabled by additive manufacturing
Adaptive self-healing materials
Complex hierarchical composites
Complex alloys
Hybrid liquid/solid systems
Ghoniem and Williams, 2017
P. Rindt, PFMC 2017
Flame spray
Wire EDM texture

## Slide 29: Outline
Plasma-Material Interaction (PMI) challenges
Potential Plasma-Facing Materials (PFMs) and Components (PFCs)
Current status of U.S. PMI research
Facilities needed for the development of PFCs
Strategic elements to accelerate U.S. burning plasma research
A proposed high-level R&D program and roadmap for PMI

## Slide 30: Status
WEST
TPE
PISCES
W7-X
EAST
LTX
World-wide unique capabilities to study Be, T effects in linear devices. They are ideal for single to few effects studies and benchmarking of PMI computational models. Leadership in PMI science. | Recently, high flux, high fluence linear devices became operational (Magnum-PSI)
Various small scale devices (LTX, HIDRA) etc. offer unique capabilities to test liquid metal PFCs in particular liquid Lithium. | Liquid metals are also studied on Magnum-PSI, FTU, TJ-II and in the future on COMPASS Upgrade.
Well diagnosed divertor plasmas. Leadership in Div/SOL science. Design of devices allows in principle for testing divertor concepts to various degrees of closure. Load-lock systems (DIMES, MAPP) allow exposure of material samples. | International devices have more relevant wall and divertor materials installed: W and Be (JET, AUG, EAST, WEST). Some devices also offer unique capabilities to test new divertors (MAST, TCV), and in future COMPASS Upgrade. Furthermore DTT in Frascati on the horizon.
In collaboration with international long pulse devices, U.S. develops actively-cooled PFCs and steady-state scenarios compatible with PFMs with respect to confinement, erosion/re-deposition (dust production), T-retention. | Obviously home institutions of steady-state toroidal devices have advantage.
Excellent tools to develop nuclear materials. Leadership in material science and neutron science. World leading neutron sources. | Capabilities spread around the world. If IFMIF or DONES will be built, leadership could move to international facilities.
U.S. PMI R&D
International PMI R&D

## Slide 31: Outline
Plasma-Material Interaction (PMI) challenges
Potential Plasma-Facing Materials (PFMs) and Components (PFCs)
Current status of U.S. PMI research
Facilities needed for the development of PFCs
Strategic elements to accelerate U.S. burning plasma research
A proposed high-level R&D program and roadmap for PMI

## Slide 32: Development of PFCs requires devices with increased capabilities to test PMI at reactor relevant level
Classical Debye vs. Chodura sheath
Non-linear evolution of surface
as well as bulk effects
Parallel impurity transport (entrainment)
Ion implantation,
fuzz
10-100 nm
Blisters
10-50 mm
Cracks
mm
Transport in plasma Transport in material

## Slide 33: Increased capabilities with MPEX
New plasma source concept (Helicon, EBW, ICRH) for independent control of Te and Ti for entire divertor plasma parameter range.
MPEX planned capabilities | 
Steady-state magnetic field [T] | 1-2
Steady-state high power flux to target [MW/m2] | > 10
Steady-state high power plasma flux on tilted (5 degree) target [MW/m2] | 3
Target Te, Ti [eV] | 1 - 15
Target ne [m-3] | 1021 - 1019
Source Te, Ti [eV] | 20-30
Reactor relevant ion flux [m-2s-1] | 1024
Annual fluence | 1031
Transients (laser, ET source, e-beam) | Under assessment
Neutron irradiated samples | Y
Test of divertor component mock-ups | Y
DEMO
MPEX
FNSF
ITER
EAST
JT60-SA
JET
DIII-D
C-mod
W erosion at 10 eV

## Slide 34: Outline
Plasma-Material Interaction (PMI) challenges
Potential Plasma-Facing Materials (PFMs) and Components (PFCs)
Current status of U.S. PMI research
Facilities needed for the development of PFCs
Strategic elements to accelerate U.S. burning plasma research
A proposed high-level R&D program and roadmap for PMI

## Slide 35: Strategic elements for U.S. PMI program
An Advanced Linear Plasma Device
Fusion Prototypic Neutron Source
Whole device modeling capability to be able to make reliable predictions on power exhaust
A DTT ??

## Slide 36: Outline
Plasma-Material Interaction (PMI) challenges
Potential Plasma-Facing Materials (PFMs) and Components (PFCs)
Current status of U.S. PMI research
Facilities needed for the development of PFCs
Strategic elements to accelerate U.S. burning plasma research
A proposed high-level R&D program and roadmap for PMI

## Slide 37: Some milestones for PMI and PFC R&D
Long term milestones within 15 years
Contribute to second generation divertor of ITER (higher heat flux > 10 MW/m2, higher fluence, few dpa)
First divertor and first wall components for US next step device (high heat flux >10 MW/m2, ~10 dpa)
Second generation divertor for US next step device (high heat flux > 20 MW/m2, high fluence, high dpa > 50dpa)
Short term milestones within 5 years
Build advanced linear plasma device MPEX
Down-selection between solid PFCs and liquid metal PFCs
Decision on need for a DTT (on basis of knowledge derived from experiments, modeling and theory).

## Slide 38: Near term R&D priority for PMI (5 years)
Develop solid material PFC technology
Scope liquid metal PFC technology
Develop advanced manufacturing methods and tools for fusion applications as PFCs (e.g. additive manufacturing, materials by design utilizing AI)
Assess free-flowing liquid metal PFCs in LTX and NSTX-U
Assess the science of evolving surfaces with high flux, high fluence linear devices
Assess hydrogen retention in candidate materials with high flux, high fluence linear devices
Assess material migration of candidate novel PFMs in existing toroidal devices
Assess power exhaust scenarios with highly radiative plasmas and novel divertors on existing toroidal devices (DIII-D and international e.g. MAST, TCV, COMPASS Upgrade, AUG, JET, EAST, WEST)
Develop integrated (whole device) modeling tools (AToM) to interpret power exhaust experiments to enable extrapolations to high magnetic field (low lq and high PSOL), essentially to required PSOL B / R

## Slide 39: Long term R&D priority for PMI (15 years)
Develop advanced materials for fusion (self healing, irradiation and erosion resistant)
Build low-cost fusion prototypic neutron source (e.g. accelerator driven neutron sources) for material development
Assess advanced materials under fusion prototypic conditions (high fluence, high flux, high irradiation damage)
Deploy next generation advanced solid or liquid PFCs to long pulse devices
Contribute to the design of the 2nd generation divertor for ITER
Deploy new PFC systems to US Next Step Device

## Slide 40: Roadmap: PMI and divertor development
Operations
Constr.
Fusion Demonstration Device/FNSF
2020
2030
2040
today
Existing linear devices
PISCES, TPE, P-MPEX, Magnum
MPEX
Operations
Construction
Solid Materials Technol.
Liquid Metal Technol.
International short pulse toroidal devices
JET, AUG, MAST, TCV
Power exhaust
National toroidal devices
LTX
NSTX-U
DIII-D
Liquid Li
Liquid metal
Power exhaust, material migration
Recovery
ITER
Operations
Construction
Construction
Operations
DTT
?
Stellarator Option
International long pulse toroidal devices
EAST, KSTAR, WEST, W7-X
Material migration, dust
Advanced Materials Technol.
Fusion prototypic neutron source
Design
Design